## Slide 1: Outline: Characterization of segmented Ge detectors
Lecturer: Hans-Jürgen Wollersheim
e-mail: h.j.wollersheim@gsi.de
web-page: https://web-docs.gsi.de/~wolle/ and click on
γ-ray camera
moving γ-ray source and Ge detector
scanner at GSI for segmented detectors

## Slide 2: The motivation behind the project
Existing technology relies on BGO scintillator technology
- Limited position resolution
- High patient dose requirement.
- Poor energy resolution only accept photopeak events.
- Will not function in large magnetic field
SPECT applications utilizing Compton Camera techniques.

## Slide 3: Which γ-ray camera to be used?
Requirements:
Excellent resolution Δx = 2 mm
Large field of view (FOV) = 8x9 cm2
www.siemens.de
Large FOV of ~20 cm diam.
Low spatial resolution 0.5-1 cm
Small FOV of 3-4 cm diam.
High spatial resolution 2-3 mm
Gem-imaging.com

## Slide 4: Gamma Camera: Individual multi-anode readout
16 wires in X axis and 16 wires in Y axis
Hamamatsu R2486 PSPMT
Photocathode = 56.25 mm
d = 76 mm t = 3 mm ρ = 7.4 g/cm3
LYSO scintillator
Lu2(1-x)Y2xSiO5
C.Domingo Pardo, N. Goel, et.al., IEEE, Vol.28, Dec. 2009
Lutetium–yttrium oxyorthosilicate

## Slide 5: Intrinsic activity of LYSO
LYSO: Lu1.8Y0.2SiO5:Ce
scintillating properties:
high density (7.1 g/cm3)
fast decay time (40 ns)
very high light output (~ 27600 ph/MeV)

## Slide 6: Which γ-ray camera to be used?
Small FOV of 3-4 cm diam.
High spatial resolution 2-3 mm
Gem-imaging.com
Requirements:
Excellent resolution Δx = 2 mm
Large field of view (FOV) = 8x9 cm2
Scintillator
Position Sensitive
PMT

## Slide 7: Which γ-ray camera to be used?
Small FOV of 3-4 cm diam.
High spatial resolution 2-3 mm
Gem-imaging.com
Requirements:
Excellent resolution Δx = 2 mm
Large field of view (FOV) = 8x9 cm2
Scintillator
Position Sensitive
PMT
g-ray

## Slide 8: Which γ-ray camera to be used?
Small FOV of 3-4 cm diam.
High spatial resolution 2-3 mm
Gem-imaging.com
Requirements:
Excellent resolution Δx = 2 mm
Large field of view (FOV) = 8x9 cm2
Scintillator
Position Sensitive
PMT
g-ray

## Slide 9: Which γ-ray camera to be used?
Small FOV of 3-4 cm diam.
High spatial resolution 2-3 mm
Gem-imaging.com
Requirements:
Excellent resolution Δx = 2 mm
Large field of view (FOV) = 8x9 cm2
Scintillator
Position Sensitive
PMT
g-ray

## Slide 10: Which γ-ray camera to be used?
Small FOV of 3-4 cm diam.
High spatial resolution 2-3 mm
Gem-imaging.com
Requirements:
Excellent resolution Δx = 2 mm
Large field of view (FOV) = 8x9 cm2
Scintillator
Position Sensitive
PMT
γ-ray
γ-ray 2

## Slide 11: Efficiency versus resolution
With a source at rest, the intrinsic resolution of the detector can be reached;
efficiency decreases with the increasing detector-source distance.
With a moving source also the effective energy resolution depends on the detector-source distance (Doppler effect)
Small d Large d
Large W Small W
High e Low e
Poor FWHM Good FWHM

## Slide 12: Energy resolution
The major factors affecting the final energy resolution (FWHM) at a particular energy are as follows:
The intrinsic resolution of the detector system.
It includes contributions from the detector itself and
the electronic components used to process the signal.
The Doppler broadening arising from the opening angle of
the detectors
The Doppler broadening arising from the angular spread of the
recoils in the target
The Doppler broadening arising from the velocity (energy)
variation of the excited nucleus

## Slide 13: Doppler broadening and position resolution
Position resolution
Angular resolution
Energy resolution
beam
projectile
g ray

## Slide 14: Segmented detectors
70cm
20cm
beam
target

## Slide 15: Gamma-ray tracking – the concept
without Compton suppression shield
with BGO shielding
with highly segmented detectors
Compton continuum → small peak to total ratio
Less solid angle coverage → big drop in efficiency
Path of γ-ray reconstructed to form full energy event
→ Compton continuum reduced
→ Excellent efficiency ~50% @ 1 MeV
→ Greatly improved angular resolution (~1%)
to reduce Doppler effect.

## Slide 16: Scanner at GSI
Characteristics:
Faster
Precision: 1-2 mm
Imaging capability
Requirements:
1. Position sensitive detector
- Excellent Δx/x
- Large field of view
2. Method to compare the pulses
Rotating table
Position sensitive detector
22Na

## Slide 17: Position calibration
Determine: Xr(xm,ym), Yr(xm,ym)
Gamma-ray scattering technique
Grid raw image when it is parallel to PSD surface (0 deg)
00 position

## Slide 18: Position reconstruction
LYSO =76 mm
Photocathode=56.26 mm
Central Interaction
Peripheral Interaction
C. Domingo Pardo, N.Goel, et.al., IEEE, Dec. 2009 Volume: 28 Issue 12
average charge profile at the center
Reference peak fitting
Charge (a.u.)
Charge (a.u.)
Y (mm)
Y (mm)
C.W.Lerche, et.al., NIM A, Vol 537, pp. 326-330, Jan. 2005

## Slide 19: Position reconstruction
Gaussian fitting
Reference peak fitting
Linear for 50 mm
Field of view = 28 cm2
Pos. X (mm)
Gaussian fitting works relatively well in the central region
Average spatial resolution in X and Y ~ 1mm
Pos. X (mm)

## Slide 20: Scanner at GSI
Characteristics:
Faster
Precision: 1-2 mm
Imaging capability
Requirements:
1. Position sensitive detector
- Excellent Δx/x
- Large field of view
2. Method to compare the pulses
Rotating table
Position sensitive detector
22Na

## Slide 21: Superiority over conventional scanner
Advantage over conventional scanner: Full detector can be scanned in one measurement 10 times faster than a conventional scanner Accuracy of simulations can be checked for complex regions of electric field
BGO
BGO
coincidence between the Germanium and BGO detectors for 90 degree Compton scattered events for depth determination
137Cs

## Slide 22: Scanner based on pulse shape comparison scan
a)
a)

## Slide 23: Scanner based on pulse shape comparison scan
a)
b)
b)
Geometric crossing point: x,y,z
Common pulse out of data sets (a) & (b)
a)
Collimated source
F.C.L. Crespi, et al. NIM A 593 (2008), 440

## Slide 24: Pulse shape comparison scan method based on a position sensitive detector
22Na
Position sensitive
detector
a)
b)
Rotated by 900
Recording pulse shapes for positions (a) and (b)
Identical signals at the crossing point.
511 keV
22Na

## Slide 25: minimization method
0° measurement
t(ns)
t(ns)
amplitude, Φ
distribution
t(ns)
amplitude, Φ
Average pulse
amplitude, Φ
threshold
90° measurement

## Slide 26: Characterization of planar HPGe detector
Front view
Side view
Planar Ge
d = 4 cm
t = 2 cm
22Na
Position sensitive detector

## Slide 27: Detector scan
Front view (0 deg):
Side view (90 deg):

## Slide 28: Detector scan
Front view (0 deg):
Side view (90 deg):

## Slide 29: Detector scan data analysis

## Slide 30: Experimental validation of the method

## Slide 31: Planar HPGe detector scan
(a)
(b)
Intensity distribution for photopeak events
t(ns)
amplitude, Φ
t(ns)

## Slide 32: AGATA: Advanced Gamma Tracking Array
4π array of germanium crystals
180 segmented crystals arranged around the reaction target
3D sensitivity
Symmetric AGATA prototype crystal

## Slide 33: Signal shapes from all 36 segments
Photopeak event
Most significant transient charge signals are from the direct neighbouring segments

## Slide 34: Combined trace for pulse shape comparison
We have the method, the device and the detector ready, lets do the scan of AGATA!
Direct neighbours of segment F3

## Slide 35: Gamma detector array
Signals from 36 segments + core
are measured as a function of time
(γ-ray interaction point)
EUROBALL Cluster Detectors
PRESPEC - AGATA
15 EUROBALL det.
photopeak eff. 2.8%

## Slide 36: New scanner at GSI
LYSO & SIPM (Silicon Photomultiplier Sensors, series C, 3mm)
www.onsemi.com/products/sensors/photodetectors-sipm-spad/silicon-photomultipliers-sipm/c-series-sipm
Advantages:
High detection probability
Disadvantages:
Dark current (temperature)
3x3 mm
single-photon avalanche diode

## Slide 37: Outlook
?
M.J. French et al., NIMA 466 (2001) 359
APV25 chip (from CERN CMS experiment)
128-channel analogue pipeline chip
The GSI system uses conventional NIM and VME electronics, which makes it not easily portable, not easily scalable and rather expensive if one wants to build many of these devices.
However, this drawback could be overcome thanks to the increasing technology of electronics, e.g. a new acquisition system based on ASIC, FPGA, etc. technologies. This would also make the system more suitable for medical applications.